- Explain why studying the types of chips produced is important in understanding cutting operations.

- Tool life can be almost infinite at low cutting speeds. Would you recommend that all machining be done at low speeds? Explain.

- Explain the consequences of allowing temperatures to rise to high levels in cutting?

- What are the effects of performing a cutting operation with a dull tool?

- An aerospace aluminum alloy has a very high thermal conductivity and strength, but cutting it results in serrated chips. What would you say about the strength of the aluminum at high temperatures?

- Why does temperature have such an important effect on the life of cutting tools?

- Can cutting fluids have any adverse effects? If so, what are they?

- Titanium-nitride coatings on tools reduce the coefficients of friction at the tool-chip interface. What is the significance of this?

- Why are chemical stability and inertness (non-reactivity) important in cutting tools?

- Thermal conductivity and coefficient of thermal expansion can be important to the life of cutting tool. Why?