Analysis of Silver in an Alloy

Purpose:  The purpose of this experiment is to determine the silver content in a silver-copper alloy.  Since neither silver nor copper are very reactive this is first done by dissolving the alloy in nitric acid.  The acid oxidizes the metals producing Ag+ and Cu+2.  The reduction product is nitrogen monoxide which reacts with oxygen in the air to form nitrogen dioxide.  Once the silver and copper are in the solution they can be separated by precipitating out the silver as silver chloride.  This insoluble solid can then be filtered out of the solution, dried and massed.

| Silver-Copper Alloy | Nitric acid (HNO3), 6 M |
| --- | --- |
| Sodium Chloride | Beakers, 100 and 250mL |
| Stirring Rod | Watch Glass |
| Hot Plate | Graduated Cylinder |
| Triple Beam Balance | Wash Bottle |
| Tongs | Fume Hood |
| Para film |  |

Materials:

Procedure:

1.  Obtain a sample of silver-allow and determine its mass precisely on a balance.

2.  Put the allow in a clean 100mL beaker and carefully pour 10 mL (for ever .5g) of 6M nitric acid over it.  Cover the beaker with the watch glass.  It may be necessary to heat the solution so the alloy totally dissolves.

3.  Calculate the amount of sodium chloride that would be necessary to precipitate the silver in your sample assuming that it is 100% silver..  use a balance to weigh out 2X this amount.  Dissolve this in approximately 25mL of distilled water.

4.  Remove the watch glass from the baker and rinse the bottom.  Slowly add the sodium chloride solution.  Stir with a stirring rod and use distilled water to rinse any solution clinging to the rod back into the beaker.

5.  Cover the beaker with Para film and allow it to stand overnight.

6.  Prepare a funnel and a piece of filter paper (make sure to weight the filter paper first).  Also prepare a wash bottle with 150mL of distilled water and 6M HNO3 to rinse the baker with as you filter.

7.  Carefully pour the solution and precipitate into the filter.  Be sure to get every particle.

8.  Leave the sample to dry overnight in a safe place.  Once dry, weigh the sample.

9.  From your data determine the percent silver in the alloy.

Calculations:

Ag + NaCl → AgCl +Na

1.  How much NaCl was used?

2.  How much AgCl was produced?

3.  What is the percent of silver in the dime?

4.  What is the percent error of the lab?

Data Table:

| Mass 1964 dime: | 2.522g |
| --- | --- |
| HNO3 Added: | 74mL HNO3 |
| NaCl Added: | 2.732g NaCl |
| Mass of Filter Paper: | 1.309g |
| Mass of Filter Paper and AgCl: | 7.309g |
| Reaction: | Ag + NaCl → AgCl + Na |
| Amount of NaCl Used: | 2.732g NaCl |
| Amount of AgCl Produced: | 6.00g |
| Percent of Ag Produced: |  |
| Percent Error: |  |

Discussion:

At first we tried to precipitate a 1964 nickel in order to find its percent of silver.  The solution did not change color when NaCl was added, and after several days we realized that the solution was not precipitating.  The solution did not precipitate because a 1964 nickel is solely composed of a 75-25 alloy.  Because of this, we had to change our experiment on a nickel to that of a dime.

During our experiment we doubled the amount of salt.  This was done because the salt is what caused the AgCl to precipitate, and we needed to make sure that as much AgCl was precipitated as possible.

There were many sources of error in the lab.  First of all, the solution was moved on and off the heat source, which could have caused less AgCl to precipitate than what we calculated.  Once the solution was placed into a paper filter traces of AgCl might have been left in the beaker and slight traces of sodium could have been among the AgCl, causing our measurements to be inaccurate.  The triple-beam balance also could have added to inaccurate weights of the paper and of the AgCl because the one we used was fairly imprecise.