- Three samples of aluminium are subjected to a constant stress and the times required to produce a constant strain of 0.1% during steady state creep at different temperatures are shown in table 1 below.

| Temperature (00C) | 151 | 205 | 258 |
| --- | --- | --- | --- |
| Time (hours) | 100 | 1.0 | 0.028 |

Use this information to determine graphically.

- The temperature at which a strain of 0.1% is produced after 10 hours.

- The activation energy for steady-state creep.